## Standard Operating Procedure: Microstructural Quantification of Emulsions, Foams, and Whipped Systems Using PhasePix

Applicable System: PhasePix Quantitative SEM Microstructure Analyzer

### 1. Purpose and Scope

This Standard Operating Procedure (SOP) defines the sequential operational workflow, parameter selection criteria, and quality control (human-in-the-loop) verification steps required to quantify air bubbles, free matrix fat globules, and interfacially adsorbed fat globules from Scanning Electron Microscopy (SEM) micrographs using PhasePix.

### 2. Pre-Analysis Preparation

- File Naming Convention: Include the nominal scale-bar length in micrometers directly in the filename (e.g., SampleA_whipped_100um_5kV.tif or _5um_). PhasePix automatically parses patterns matching *um to pre-populate the physical calibration.

- Image Placement: Place raw micrographs (.tif, .tiff, .png, .jpg, .bmp) into the local images/ directory or upload them directly via the browser interface.

### 3. Step-by-Step Operational Sequence

#### Step 1: Image Loading and Footer Exclusion (Sidebar Sections 1–2)

- Select the image source method (From 'images/' folder or Upload via Browser) and load the target micrograph.

- Set Footer Height (pixels) (default: 70 px).

  - Recommendation: Ensure the dimmed band at the bottom of the micrograph completely covers the SEM information banner (voltage, magnification, scale bar text) without cropping into the sample region. Adjust in 5 px increments if using a different SEM instrument format.

#### Step 2: Spatial Calibration Verification (Sidebar Section 3)

- Inspect the Detected scale-bar line preview image in the sidebar. Confirm that the red vertical tick marks accurately bracket the two ends of the SEM scale bar.

- Verify Real Scale Bar Size (µm) and Scale Bar Length (pixels).

  - Fallback Action: If the SEM banner uses a non-standard layout and automatic detection fails, switch to the 📏 Visual Ruler tab, set scale_bar_um = scale_bar_length_px temporarily (1:1 px), measure the scale bar line manually, and enter the exact pixel length into Scale Bar Length (pixels).

#### Step 3: Unknown Feature Sizing via Visual Ruler (Tab: 📏 Visual Ruler)

Before setting size boundaries for a new formulation or magnification:

- Open the 📏 Visual Ruler tab.

- Click and drag caliper lines across the smallest fat globule, the largest fat globule/cluster, and representative air bubbles.

- Record the measured lengths in micrometers (μm) displayed in the right-hand panel.

#### Step 4: Phase Classification & AI Detection Setup (Sidebar Sections 4–5)

Select the Sample Type (Emulsion, Whipped Emulsion, or Foam) and configure parameters according to the table below:

| Parameter | Low Magnification Overview (e.g., 500x – 1,500x; Scale bar 50–200 µm) | High Magnification Detail (e.g., 5,000x – 15,000x; Scale bar 2–10 µm) | Operational Recommendation & Physical Rationale |
| --- | --- | --- | --- |
| AI Detection Target (Whipped Emulsion) | 🫧+🟠 Both Air Bubbles & Fat Particles (Two-Pass) (or 🫧 Air Bubbles Only for rapid foam screening) | 🫧+🟠 Both Air Bubbles & Fat Particles (Two-Pass) | Always use Two-Pass when quantifying Pickering stabilization or matrix coalescence alongside air cells. |
| Air Bubble Size Range (µm) | Min: 10.0 µm to Max: 150.0 µm | Min: 3.0 µm to Max: 40.0 µm | Set slightly wider than caliper measurements to avoid rejecting valid deformed pores. |
| Fat Particle Size Range (µm) | Min: 0.40 µm to Max: 5.0 µm | Min: 0.15 µm to Max: 3.5 µm | Defines both the size gate and the automatic Cellpose target diameter (deff=1.25⋅dmin,fat/Rμm/px). |
| Pretrained Model | cyto2 | cyto2 | Generalist cytoplasmic model optimal for spherical/ovoid colloidal structures. |
| flow_threshold | 0.70 (Default) | 0.75 – 0.85 | Increase to 0.80 if partially coalesced or irregular globules are missed; decrease to 0.50 if background noise creates false shapes. |
| cellprob_threshold | -1.0 (Default) | -1.5 to -2.5 | Lower (more negative) values force detection of faint, low-contrast pores and shadowed globules. |
| 🫧 Air Bubbles Min Circularity | 0.50 | 0.40 | Lower to 0.35–0.40 if air cells are elongated/sheared during whipping. |
| 🟧 Matrix Fat Min Circularity | 0.60 | 0.55 – 0.65 | Filters out non-globular fracture debris in the continuous matrix. |
| 🟨 Adsorbed Fat Min Circularity | 0.30 | 0.25 – 0.35 | Must remain low (0.30) because globules protruding from curved crater walls appear hemispherical or crescent-shaped in 2D projection. |
| 🔬 Deep-Scan Adsorbed Fat | Checked (True) for final analysis; Unchecked for initial preview | Checked (True) | Runs Pass 3/3 localized shadow-recovery (percentile stretch + γ=0.85 + CLAHE) inside air craters. |
| Enable CLAHE Preprocessing | Checked (True) | Checked (True) | Boosts local edge gradients before neural network inference. |

Click 🔄 Apply Size Ranges & Classification after modifying size ranges.

#### Step 5: Human-in-the-Loop Verification & Manual Correction (Tab: 🖌️ Manual Correction)

- Switch to the 🖌️ Manual Correction tab. Collapse the left sidebar (<<) to inspect the canvas at 100% native 1:1 resolution.

- Automated air bubbles are displayed with a thin teal outline. Identify any missed air bubbles, irregular coalesced air channels, or missed fat globules.

- Choose the appropriate Selection Method based on feature visibility:

  - 📐 Exact Smooth Curve by Points: Recommended for complex, shadowed, or rim-decorated air bubbles. Click points sequentially along the true physical perimeter of the crater and click ➕ Add Manual Bubble. PhasePix constructs a periodic cubic spline passing 100% through your clicked coordinates (0.0 px shift).

  - 📦 AI Smart Box: Recommended for fully visible, well-defined particles or pores. Drag a tight rectangle around the object and click ➕ Detect & Add from Box(es).

  - 🪄 1-Click Dark Pore Center: Recommended for rapid addition of simple dark circular pores. Click once inside the dark core and click ➕ Add Bubble.

- Set Assign New Manual Objects As (air_bubbles, fat_particles, or adsorbed_fat) prior to committing.

- Mandatory Persistence Step: Scroll to 💾 Manual Mask Persistence and click 💾 Save Manual Objects to Disk. This writes images/<filename>_manual_masks.json, protecting manual work against session resets.

#### Step 6: Phase Cleaning & Smart Bulk Actions (Tab: 📊 Interactive Dashboard)

- Return to 📊 Interactive Dashboard.

- Inspect green objects (Unclassified) on the overlay:

  - If Unclassified objects are valid globules slightly outside the nominal size range, click ✨ Smart Auto-Split All (automatically assigns objects inside bubbles to adsorbed_fat and outside to fat_particles).

  - If Unclassified objects are charging artifacts or ice crystals, click 🗑️ Delete All Unclassified.

  - To remove individual artifacts, check the Excluded box in the 2. Phase Classifications table and click Apply Changes.

#### Step 7: Interfacial Adsorption Analysis (Tab: 🛡️ Interfacial Analytics)

- Open the 🛡️ Interfacial Analytics tab.

- Examine the 🖼️ Selected Bubble Inspection Overlay, where each bubble is labeled at its center with its white numeric ID.

- Quality Control Filtering: In 🎯 Select Verified Air Bubbles for Interfacial Analysis (ID), remove the IDs of any bubbles that are severely truncated by the image border, out of focus, or occluded by fracture debris. Retain only verified bubbles where adsorbed globules are clearly resolved.

- Select the Reference Fat Globule Diameter (Dref) mode:

  - Use Mean Matrix Fat Diameter for standard statistical comparison.

  - Use Matrix Fat Sauter D[3,2] when surface-area weighted scaling is preferred.

  - Use Custom Value (µm) when analyzing high-magnification images of a single bubble where no free matrix fat is visible in the frame (enter the known mean fat diameter from a corresponding emulsion/matrix image).

- Use the 🔍 Single Bubble Crop Inspector to inspect individual bubbles closely and download specific Bubble Crop (PNG) and Bubble Protocol (CSV) files.

#### Step 8: Matrix Partial Coalescence Analysis (Tab: 🍇 Matrix Coalescence)

- Open the 🍇 Matrix Coalescence tab.

- If the micrograph contains shadowed regions or charging zones where matrix fat detection is incomplete, check 🎯 Analyze Specific Verified Sub-Region (ROI Box) of Matrix and adjust the Horizontal/Vertical ROI Range (%) sliders to isolate a clean, representative region of the continuous matrix.

- Set Inter-Globule Contact Bridge Tolerance (px) (default: 3 px).

  - Recommendation: Keep at 2–3 px for standard resolution; increase to 4–5 px only at very high magnifications (≥15,000×) where Cellpose mask boundaries leave a slight pixel gap across sintered fat necks.

#### Step 9: Data Export & Archiving

- Export phase distributions and granulometry tables from 📊 Interactive Dashboard and 🔬 Metrics.

- Export adsorption summaries, per-bubble metrics, and contact-angle distributions from 🛡️ Interfacial Analytics.

- Export coalescence summaries, network maps, Z-distributions, and cluster tables from 🍇 Matrix Coalescence.

- Open 💾 Reproducibility & Export and click 📥 Download Manifest (.txt) to archive all exact model thresholds, spatial calibration factors, and phase counts alongside your experimental data.